How to charge Thunder Power Li-Polymer batteries.

1) Measure battery voltage before charging.

Voltage before charging		Status

2SxP		6V or higher		Good condition

3SxP		9V or higher 		Good condition

4SxP		12V or higher 		Good condition

2) Select number of cells or appropriate voltage.

2SxP = 2 cells or select 7.4V

3SxP = 3 cells or select 11.1V

4SxP = 4 cells or select 14.8V

3) Select charge current.

If not listed, limit charge current to 1C!!!

Capacity 		Charge current

730mAh		700-750mAh

880mAh		700-900mAh

1200mAh		1000-1300mAh

1300mAh		1000-1300mAh

1950mAh		1500-2000mAh

2050mAh		1500-2000mAh

2600mAh		2000-2600mAh

6000mAh		2000-6000mAh

7800mAh		2000-8000mAh

8200mAh		2000-8000mAh

4) Check your charger for safety.

a) After charging, check the battery with Voltmeter, the voltage should be:

Cell count:		Fully charge voltage:

2 cells pack		8.32-8.45V

3 cells pack		12.48-12.68V

4 cells pack		16.64-16.90V

b) For Triton charger reset timer to 5 hours.

c) Do not use Orbit charger with 6.1 firmware (selecting wrong cell count can cause                              fire)

4) Let the battery cool down to ambient temperature before charging.

5) Charging batteries in series.

- Battery packs must have the same level of discharge (within 0.1V for 3S4P and 4S4P)

- Battery pack must be fully charged before use.

6) Storage.

- Never store your battery inside of your car in extreme temperatures.

- Do not expose battery pack to direct sunlight for extended period.

- Do not discharge below 3V per cell.